Supervised machine learning for predicting and explaining macrophage cytokine responses to hydrogels

Yanbing Liua, Yaxi Chena,b, Hongyi Chenc, Lan Wangd, Jie Huanga,*

a Department of Mechanical Engineering, University College London, London, UK

b Hawkes Institute, University College London, London, UK

c Department of Computer Science, University College London, London, UK

d Aier Eye Institute, AIER Eye Hospital Group, Changsha, PR China

*Corresponding author: Jie Huang (jie.huang@ucl.ac.uk)

| Feature | Type | Unit or coding | Definition |
| --- | --- | --- | --- |
| hydrogel composition | Categorical | A–C | Origin of structural network-forming constituents: natural polymer, synthetic polymer, or natural–synthetic hybrid. Modified natural backbones remain natural; cargo alone does not determine origin. |
| modulus | Numerical | kPa | Recorded mechanical modulus, converted to kPa; includes storage, compressive and other reported modulus types. |
| pore size | Numerical | µm | Characteristic hydrogel pore size, as reported or digitised from the source. |
| bioactive cue | Categorical | A–F | Material-associated immune or pro-regenerative signalling cue; distinct from external activation. Categories describe supported roles, not cytokine magnitude or literal growth-factor cargo. |
| crosslink method | Categorical | A–D | Harmonised network-formation mechanism. Temperature-triggered physical gelation is included in physical self-assembly; other chemical or mixed routes remain in the residual category. |
| crosslink level | Categorical | A–C | Qualitative network classification using the criteria in Table S2. |
| macrophage model | Categorical | A–E | Macrophage cell model or primary/tissue context used for the cytokine measurement. |
| activation stimulus | Categorical | A–F | Externally applied stimulation context, including unstimulated or basal conditions. |
| exposure mode | Categorical | A–F | Hydrogel–cell interaction or assay geometry, including porous scaffold residence, indirect exposure and in vivo endpoints. |
| exposure time | Numerical | h | Recorded duration of culture or material exposure; distinct from material preparation or prior LPS priming. |

Table S1a. Definitions of the model features.

| Feature | Categorical coding |
| --- | --- |
| hydrogel composition | A, natural polymer; B, natural–synthetic hybrid; C, synthetic polymer |
| bioactive cue | A, none; B, anti-inflammatory cue; C, anti-inflammatory + pro-regenerative signalling cues; D, pro-regenerative signalling cue; E, pro- and anti-inflammatory cues; F, pro-inflammatory cue |
| crosslink method | A, photo-crosslinking; B, physical self-assembly; C, enzymatic crosslinking; D, other / mixed |
| crosslink level | A, medium; B, high; C, low |
| macrophage model | A, RAW264.7; B, murine primary or in vivo context; C, THP-1; D, human monocyte-derived macrophages; E, bone-marrow-derived macrophages |
| activation stimulus | A, LPS; B, unstimulated or basal; C, IL-4/IL-13; D, LPS + IFN-γ; E, other stimulation; F, unclear |
| exposure mode | A, direct surface contact; B, hydrogel extract or eluate; C, 3D encapsulation / scaffold residence; D, in vivo tissue or systemic; E, Transwell or indirect; F, unclear |

Table S1b. Categorical codes used in the dataset tables. Codes are nominal labels, ordered by pooled frequency in Tables S8-S9, with other/mixed and unclear categories placed last.

| Scoring dimension | Score = 0 | Score = 1 | Score = 2 |
| --- | --- | --- | --- |
| Network complexity | Single weak physical network | Single stable network or single chemical network | Double network, multiple crosslinking mechanisms, or combined physical and chemical crosslinking |
| Crosslink-density clues | Clearly low crosslink density | Conventional or moderate crosslink density | Clearly high crosslink density |
| Mechanical/structural stability clues | Soft, loose, weakly stable, or rapidly swelling/degrading | Intermediate mechanical strength or stability | Reinforced, highly stable, dense, or low-swelling network |
| Source-author wording | Terms such as loosely crosslinked, soft, or weak | No clear tendency reported | Terms such as dense, reinforced, robust, or strong |

Table S2. Scoring criteria for crosslink level classification.

| Feature | TNF-α available n (%) | TNF-α missing n (%) | IL-10 available n (%) | IL-10 missing n (%) |
| --- | --- | --- | --- | --- |
| hydrogel composition | 139 (100.0%) | 0 (0.0%) | 133 (100.0%) | 0 (0.0%) |
| modulus | 105 (75.5%) | 34 (24.5%) | 97 (72.9%) | 36 (27.1%) |
| pore size | 112 (80.6%) | 27 (19.4%) | 104 (78.2%) | 29 (21.8%) |
| bioactive cue | 139 (100.0%) | 0 (0.0%) | 133 (100.0%) | 0 (0.0%) |
| crosslink method | 139 (100.0%) | 0 (0.0%) | 133 (100.0%) | 0 (0.0%) |
| crosslink level | 139 (100.0%) | 0 (0.0%) | 133 (100.0%) | 0 (0.0%) |
| macrophage model | 139 (100.0%) | 0 (0.0%) | 133 (100.0%) | 0 (0.0%) |
| activation stimulus | 139 (100.0%) | 0 (0.0%) | 133 (100.0%) | 0 (0.0%) |
| exposure mode | 139 (100.0%) | 0 (0.0%) | 133 (100.0%) | 0 (0.0%) |
| exposure time | 133 (95.7%) | 6 (4.3%) | 129 (97.0%) | 4 (3.0%) |

Table S3a. Availability of the ten model features before imputation.

| Excluded feature | TNF-α reporting evidence | IL-10 reporting evidence | Exclusion reason |
| --- | --- | --- | --- |
| swelling ratio | 14/41 studies (34.1%) | 16/36 studies (44.4%) | Reference mass, medium and equilibration time differ; a common numerical swelling descriptor is not established. |
| porosity | 3/41 studies (7.3%) | 6/36 studies (16.7%) | Void fraction, section area fraction and pore dimensions must remain distinct; comparable row-level values are incompletely resolved. |
| quantitative bioactive-cue loading | 15/41 studies (36.6%) | 10/36 studies (27.8%) | Feed amount, carrier loading, retained payload and delivered exposure dose use different denominators; they cannot be pooled without assumptions. |
| stress-relaxation measurements | 1/41 studies (2.4%) | 1/36 studies (2.8%) | One study reported relaxation curves; no common relaxation-time scalar was available. |
| degradation kinetics or time | 19/41 studies (46.3%) | 16/36 studies (44.4%) | Reported measures included mass loss, erosion, imaging retention and complete degradation time under different media and endpoints; no common kinetic descriptor was available. |
| mesh size (theoretical) | 2/41 studies (4.9%) | 2/36 studies (5.6%) | Available values were theory-derived network lengths rather than imaged pores, with insufficient comparable row-level measurements. |

Table S3b. Study-level reporting of descriptors not included in the models.

| No. | Cytokine | Imputation method | Model | R² | RMSE (pg/mL) | MAE (pg/mL) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | TNF-α | Median | LightGBM | 0.700 | 259.68 | 177.14 |
| 2 | TNF-α | Median | Gradient boosting regression | 0.718 | 251.75 | 171.88 |
| 3 | TNF-α | Median | XGBoost | 0.700 | 259.71 | 176.81 |
| 4 | TNF-α | Median | Random forest | 0.656 | 278.32 | 185.45 |
| 5 | TNF-α | Mean | LightGBM | 0.518 | 329.05 | 218.87 |
| 6 | TNF-α | Mean | Gradient boosting regression | 0.582 | 306.59 | 208.68 |
| 7 | TNF-α | Mean | XGBoost | 0.573 | 310.00 | 215.77 |
| 8 | TNF-α | Mean | Random forest | 0.655 | 278.62 | 191.79 |
| 9 | TNF-α | Iterative Bayesian ridge | LightGBM | 0.454 | 350.25 | 224.15 |
| 10 | TNF-α | Iterative Bayesian ridge | Gradient boosting regression | 0.527 | 325.98 | 210.33 |
| 11 | TNF-α | Iterative Bayesian ridge | XGBoost | 0.556 | 316.19 | 213.35 |
| 12 | TNF-α | Iterative Bayesian ridge | Random forest | 0.588 | 304.50 | 201.25 |
| 13 | TNF-α | Scaled KNN (k = 3) | LightGBM | 0.586 | 305.29 | 203.01 |
| 14 | TNF-α | Scaled KNN (k = 3) | Gradient boosting regression | 0.620 | 292.40 | 198.64 |
| 15 | TNF-α | Scaled KNN (k = 3) | XGBoost | 0.624 | 290.78 | 195.67 |
| 16 | TNF-α | Scaled KNN (k = 3) | Random forest | 0.592 | 303.06 | 199.95 |
| 17 | TNF-α | Scaled KNN (k = 5) | LightGBM | 0.589 | 303.92 | 206.30 |
| 18 | TNF-α | Scaled KNN (k = 5) | Gradient boosting regression | 0.602 | 299.32 | 201.14 |
| 19 | TNF-α | Scaled KNN (k = 5) | XGBoost | 0.605 | 298.00 | 204.45 |
| 20 | TNF-α | Scaled KNN (k = 5) | Random forest | 0.596 | 301.41 | 198.22 |

Table S4a. Comparison of numerical imputation methods for TNF-α prediction.

| No. | Cytokine | Imputation method | Model | R² | RMSE (pg/mL) | MAE (pg/mL) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | IL-10 | Median | LightGBM | 0.695 | 212.95 | 129.05 |
| 2 | IL-10 | Median | Gradient boosting regression | 0.724 | 202.32 | 125.40 |
| 3 | IL-10 | Median | XGBoost | 0.733 | 199.10 | 126.50 |
| 4 | IL-10 | Median | Random forest | 0.749 | 192.83 | 117.88 |
| 5 | IL-10 | Mean | LightGBM | 0.714 | 205.95 | 126.72 |
| 6 | IL-10 | Mean | Gradient boosting regression | 0.761 | 188.32 | 118.77 |
| 7 | IL-10 | Mean | XGBoost | 0.770 | 184.62 | 121.64 |
| 8 | IL-10 | Mean | Random forest | 0.766 | 186.43 | 108.96 |
| 9 | IL-10 | Iterative Bayesian ridge | LightGBM | 0.689 | 214.75 | 126.34 |
| 10 | IL-10 | Iterative Bayesian ridge | Gradient boosting regression | 0.731 | 199.97 | 120.93 |
| 11 | IL-10 | Iterative Bayesian ridge | XGBoost | 0.763 | 187.40 | 118.60 |
| 12 | IL-10 | Iterative Bayesian ridge | Random forest | 0.778 | 181.53 | 108.03 |
| 13 | IL-10 | Scaled KNN (k = 3) | LightGBM | 0.625 | 236.05 | 136.56 |
| 14 | IL-10 | Scaled KNN (k = 3) | Gradient boosting regression | 0.754 | 191.21 | 118.04 |
| 15 | IL-10 | Scaled KNN (k = 3) | XGBoost | 0.728 | 200.91 | 130.14 |
| 16 | IL-10 | Scaled KNN (k = 3) | Random forest | 0.726 | 201.56 | 119.73 |
| 17 | IL-10 | Scaled KNN (k = 5) | LightGBM | 0.683 | 217.08 | 122.82 |
| 18 | IL-10 | Scaled KNN (k = 5) | Gradient boosting regression | 0.752 | 191.68 | 117.93 |
| 19 | IL-10 | Scaled KNN (k = 5) | XGBoost | 0.709 | 207.90 | 129.69 |
| 20 | IL-10 | Scaled KNN (k = 5) | Random forest | 0.705 | 209.09 | 122.28 |

Table S4b. Comparison of numerical imputation methods for IL-10 prediction.

| Cytokine | Model | Training observations | Mean ± SD R² | Mean ± SD RMSE (pg/mL) | Mean ± SD MAE (pg/mL) |
| --- | --- | --- | --- | --- | --- |
| TNF-α | Gradient boosting regression | 111 | 0.718 ± 0.007 | 251.75 ± 3.19 | 171.88 ± 3.68 |
| IL-10 | Random forest | 106 | 0.778 ± 0.001 | 181.53 ± 0.48 | 108.03 ± 0.26 |

Table S4c. Ten-fold validation performance of the selected TNF-α and IL-10 models.

| Parameter | TNF-α model | IL-10 model |
| --- | --- | --- |
| Regression model | GradientBoostingRegressor | RandomForestRegressor |
| Numerical imputation | Median | IterativeImputer with BayesianRidge |
| Categorical imputation | Constant: __missing__ | Constant: **missing** |
| Categorical encoding | Dense one-hot; unknown categories ignored | Dense one-hot; unknown categories ignored |
| Loss/objective | Squared error | Squared error |
| Tree split criterion | friedman_mse | squared_error |
| Number of estimators | 1000 | 250 |
| Learning rate | 0.08 | — |
| Maximum tree depth | 3 | 9 |
| Maximum leaves per tree | Unrestricted | Unrestricted |
| Minimum observations per leaf | 8 | 1 |
| Minimum observations to split | 2 | 2 |
| Boosting row subsampling | 0.7 | — |
| Bootstrap sampling | — | False |
| Feature sampling per split | All features | 0.7 |
| Minimum impurity decrease | 0 | 0 |
| Cost-complexity pruning (ccp_alpha) | 0 | 0 |
| Model realisations | 3 | 3 |
| Training / Test observations | 111 / 28 | 106 / 27 |
| Train/Test partition | Fixed 80:20 membership | Fixed 80:20 membership |
| Validation folds | 10 shuffled folds | 10 shuffled folds |
| Validation partition | Shared Training folds | Shared Training folds |
| Iterative imputer initialisation | — | Mean; ascending feature order |
| Iterative imputer iterations / tolerance | — | 20 / 0.001 |
| Imputer posterior sampling | — | False |
| Bayesian ridge iterations / tolerance | — | 300 / 0.001 |
| Bayesian ridge priors | — | alpha_1 = alpha_2 = lambda_1 = lambda_2 = 10⁻⁶ |
| Predictive numerical standardisation | None | None |
| Parallel jobs | — | 1 |

Table S5. Settings of the selected TNF-α and IL-10 models.

| No. | Representative | hydrogel composition | modulus (kPa) | pore size (µm) | bioactive cue | crosslink method | crosslink level | Predicted TNF-α (pg/mL) | Predicted IL-10 (pg/mL) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | P1 | natural polymer | 0.227 | 5.40947 | anti-inflammatory + pro-regenerative signalling cues | physical self-assembly | medium | 17.99 ± 14.38 | 1010.16 ± 18.92 |
| 2 | — | natural polymer | 0.280058 | 5.40947 | anti-inflammatory + pro-regenerative signalling cues | physical self-assembly | medium | 17.99 ± 14.38 | 1010.16 ± 18.92 |
| 3 | — | natural polymer | 0.3 | 5.40947 | anti-inflammatory + pro-regenerative signalling cues | physical self-assembly | medium | 17.99 ± 14.38 | 1010.16 ± 18.92 |
| 4 | — | natural polymer | 2.64817 | 3 | none | enzymatic crosslinking | medium | 64.49 ± 14.59 | 1151.97 ± 7.84 |
| 5 | — | natural polymer | 0.426277 | 3 | none | enzymatic crosslinking | medium | 101.18 ± 22.20 | 1186.52 ± 7.35 |
| 6 | — | natural polymer | 0.426277 | 3 | none | enzymatic crosslinking | medium | 104.03 ± 14.52 | 1192.71 ± 0.00 |
| 7 | — | natural polymer | 2.64817 | 84.437 | anti-inflammatory + pro-regenerative signalling cues | photo-crosslinking | low | 650.76 ± 78.23 | 1264.15 ± 2.93 |
| 8 | — | natural polymer | 2.64817 | 84.437 | anti-inflammatory + pro-regenerative signalling cues | photo-crosslinking | low | 678.61 ± 88.78 | 1268.12 ± 5.13 |
| 9 | — | natural polymer | 3.004 | 84.437 | anti-inflammatory + pro-regenerative signalling cues | other / mixed | high | 842.40 ± 145.41 | 1342.35 ± 48.07 |
| 10 | — | natural polymer | 3.004 | 84.437 | anti-inflammatory + pro-regenerative signalling cues | other / mixed | high | 878.84 ± 135.01 | 1351.24 ± 45.05 |
| 11 | P2 | natural polymer | 3.004 | 84.437 | anti-inflammatory + pro-regenerative signalling cues | photo-crosslinking | low | 1089.83 ± 131.17 | 1392.28 ± 28.38 |
| 12 | — | natural polymer | 3.004 | 84.437 | anti-inflammatory + pro-regenerative signalling cues | photo-crosslinking | low | 1118.91 ± 144.42 | 1401.64 ± 24.97 |
| 13 | — | natural polymer | 3.004 | 84.437 | anti-inflammatory + pro-regenerative signalling cues | photo-crosslinking | high | 1172.77 ± 112.90 | 1466.40 ± 35.45 |
| 14 | — | natural polymer | 3.004 | 84.437 | anti-inflammatory + pro-regenerative signalling cues | photo-crosslinking | high | 1219.68 ± 106.55 | 1475.29 ± 32.23 |
| 15 | — | natural polymer | 3.004 | 84.437 | anti-inflammatory + pro-regenerative signalling cues | other / mixed | high | 1705.90 ± 48.67 | 1608.16 ± 52.00 |
| 16 | P3 | natural polymer | 3.004 | 84.437 | anti-inflammatory + pro-regenerative signalling cues | photo-crosslinking | high | 2130.14 ± 2.29 | 1779.44 ± 0.53 |

Table S6a. Material descriptors and predicted cytokine concentrations for the 16 Pareto profiles shown in Fig. 10. P1–P3 denote the representative designs.

| Profile No. | Macrophage model | Activation stimulus | Exposure mode | Exposure time (h) |
| --- | --- | --- | --- | --- |
| 1 | RAW264.7 | LPS | hydrogel extract or eluate | 24 |
| 2 | RAW264.7 | LPS | hydrogel extract or eluate | 24 |
| 3 | RAW264.7 | LPS | hydrogel extract or eluate | 24 |
| 4 | murine primary or in vivo context | LPS + IFN-γ | direct surface contact | 36 |
| 5 | murine primary or in vivo context | LPS + IFN-γ | direct surface contact | 24 |
| 6 | murine primary or in vivo context | LPS + IFN-γ | direct surface contact | 36 |
| 7 | murine primary or in vivo context | other stimulation | direct surface contact | 36 |
| 8 | murine primary or in vivo context | other stimulation | direct surface contact | 24 |
| 9 | murine primary or in vivo context | other stimulation | direct surface contact | 36 |
| 10 | murine primary or in vivo context | other stimulation | direct surface contact | 24 |
| 11 | murine primary or in vivo context | other stimulation | direct surface contact | 36 |
| 12 | murine primary or in vivo context | other stimulation | direct surface contact | 24 |
| 13 | murine primary or in vivo context | other stimulation | direct surface contact | 36 |
| 14 | murine primary or in vivo context | other stimulation | direct surface contact | 24 |
| 15 | RAW264.7 | LPS | hydrogel extract or eluate | 24 |
| 16 | RAW264.7 | LPS | hydrogel extract or eluate | 24 |

Table S6a (continued). Experimental descriptors for the same profiles.

| Profile No. | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TNF-α domain ratio | 0.667 | 0.666 | 0.666 | 0.377 | 0.371 | 0.324 | 0.841 | 0.834 | 0.851 | 0.876 | 0.842 | 0.835 |
| IL-10 domain ratio | 0.579 | 0.579 | 0.579 | 0.334 | 0.370 | 0.333 | 0.761 | 0.757 | 0.904 | 0.900 | 0.761 | 0.757 |
| Non-dominance frequency | 6/9 | 6/9 | 6/9 | 9/9 | 6/9 | 9/9 | 7/9 | 7/9 | 9/9 | 9/9 | 9/9 | 9/9 |

Table S6b. Applicability-domain ratios and non-dominance frequency for the profiles in Table S6a.

| Profile No. | 13 | 14 | 15 | 16 | — | — | — | — | — | — | — | — |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TNF-α domain ratio | 0.732 | 0.724 | 0.617 | 0.416 | — | — | — | — | — | — | — | — |
| IL-10 domain ratio | 0.711 | 0.706 | 0.551 | 0.281 | — | — | — | — | — | — | — | — |
| Non-dominance frequency | 9/9 | 9/9 | 9/9 | 9/9 | — | — | — | — | — | — | — | — |

Table S6b (continued). Profiles 13–16.

| Feature | PEG microgel scaffold | PEG microgel scaffold with tethered IL-10 | HPA@SIN-GM | HPA@SIN-GM@DR |
| --- | --- | --- | --- | --- |
| hydrogel composition | synthetic polymer | synthetic polymer | natural polymer | natural polymer |
| modulus (kPa) | — | — | 10.0 | 10.0 |
| pore size (µm) | 90.0 | 90.0 | 7.5 | 7.5 |
| bioactive cue | none | anti-inflammatory cue | anti-inflammatory cue | anti-inflammatory + pro-regenerative signalling cues |
| crosslink method | other / mixed | other / mixed | physical self-assembly | physical self-assembly |
| crosslink level | medium | medium | high | high |
| macrophage model | THP-1 | THP-1 | RAW264.7 | RAW264.7 |
| activation stimulus | unstimulated or basal | unstimulated or basal | LPS | LPS |
| exposure mode | 3D encapsulation / scaffold residence | 3D encapsulation / scaffold residence | hydrogel extract or eluate | hydrogel extract or eluate |
| exposure time (h) | 72.0 | 72.0 | 24.0 | 24.0 |

Table S7a. Formulation features in the case studies.

| Formulation | Experimental TNF-α | Predicted TNF-α | Experimental IL-10 | Predicted IL-10 |
| --- | --- | --- | --- | --- |
| PEG microgel scaffold | 704.545 | 422.555 ± 67.820 | 208.522 | 441.690 ± 27.399 |
| PEG microgel scaffold with tethered IL-10 | 428.030 | 190.882 ± 92.441 | 552.807 | 486.719 ± 31.400 |
| HPA@SIN-GM | 612.000 [474.434, 749.566] | 590.973 ± 17.052 | 155.000 [128.525, 181.475] | 194.933 ± 6.200 |
| HPA@SIN-GM@DR | 488.963 [369.010, 668.273] | 487.348 ± 9.696 | 188.060 [166.418, 206.716] | 228.321 ± 11.957 |

Table S7b. Experimental and predicted cytokine concentrations (pg/mL).

| DOI | No. | Hydrogel composition | Modulus (kPa) | Pore size (µm) | Bioactive cue | Crosslink method | Crosslink level | Macrophage model | Activation stimulus | Exposure mode | Exposure time (h) | Measured TNF-α (pg/mL) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 10.1016/j.bioactmat.2024.07.015 | 1 | A | — | 182.8023 | A | D | A | A | F | A | 48.0 | 500.822 |
| 10.1016/j.bioactmat.2024.07.015 | 2 | A | — | 182.8023 | A | D | A | A | F | A | 96.0 | 502.583 |
| 10.1016/j.mtbio.2025.101686 | 3 | A | 19.1869 | 40.011 | A | A | A | A | A | B | 48.0 | 681.006 |
| 10.1016/j.mtbio.2025.101686 | 4 | A | 16.8094 | 50.25 | C | A | A | A | A | B | 48.0 | 675.825 |
| 10.1016/j.mtbio.2025.101686 | 5 | A | 13.1193 | 97.387 | C | A | A | A | A | B | 48.0 | 206.09 |
| 10.1038/s41467-024-50072-y | 6 | A | — | — | A | A | C | B | B | A | 24.0 | 66.2712 |
| 10.1038/s41467-024-50072-y | 7 | A | — | — | A | A | C | B | D | A | 24.0 | 274.539 |
| 10.1038/s41467-024-50072-y | 8 | A | — | — | A | A | C | B | E | A | 24.0 | 135.318 |
| 10.1038/s41467-024-50072-y | 9 | A | — | — | A | A | B | B | B | A | 24.0 | 66.2943 |
| 10.1038/s41467-024-50072-y | 10 | A | — | — | A | A | B | B | D | A | 24.0 | 613.67 |
| 10.1038/s41467-024-50072-y | 11 | A | — | — | A | A | B | B | E | A | 24.0 | 531.629 |
| 10.1186/s12951-024-02996-2 | 12 | A | 12.263 | 142.614 | B | A | B | B | C | A | 24.0 | 9.45985 |
| 10.1186/s12951-024-02996-2 | 13 | A | 16.1507 | 139.205 | B | A | B | B | C | A | 24.0 | 7.39738 |
| 10.1186/s12951-024-02996-2 | 14 | A | 29.6548 | 117.045 | C | A | B | B | C | A | 24.0 | 2.28207 |
| 10.1002/smll.202203680 | 15 | A | 0.0841 | — | A | B | C | B | E | C | 72.0 | 204.7 |
| 10.1002/smll.202203680 | 16 | A | 0.4281 | — | A | D | B | B | E | C | 72.0 | 190.5 |
| 10.1002/smll.202203680 | 17 | A | 0.4434 | — | A | D | B | B | E | C | 72.0 | 193.6 |
| 10.1002/smll.202203680 | 18 | A | 0.438 | — | A | D | B | B | E | C | 72.0 | 196.1 |
| 10.34133/bmr.0029 | 19 | A | 26.67 | 60.0 | A | D | A | A | F | F | — | 253.053 |
| 10.34133/bmr.0029 | 20 | A | 36.67 | 60.0 | A | D | A | A | F | F | — | 191.66 |
| 10.1021/acsami.2c08593 | 21 | A | 3.008 | 158.438 | A | B | C | B | E | D | 96.0 | 87.3506 |
| 10.1021/acsami.2c08593 | 22 | A | 2.265 | 44.628 | B | B | C | B | E | D | 96.0 | 54.1627 |
| 10.3389/fimmu.2023.1170153 | 23 | A | 0.752 | — | A | C | C | B | E | D | 72.0 | 632.568 |
| 10.1016/j.biomaterials.2024.122706 | 24 | B | 0.319 | 30.3213 | A | B | A | A | A | A | 48.0 | 641.249 |
| 10.1016/j.biomaterials.2024.122706 | 25 | B | 0.638 | 48.5321 | B | B | A | A | A | A | 48.0 | 529.351 |
| 10.1039/d4bm01623h | 26 | C | 10.9 | — | B | A | B | C | F | A | 144.0 | 18.4211 |
| 10.1016/j.actbio.2025.03.015 | 27 | B | 5.593 | 250.31 | A | A | B | A | A | A | 24.0 | 591.268 |
| 10.1016/j.actbio.2025.03.015 | 28 | B | 4.123 | 116.52 | B | A | B | A | A | A | 24.0 | 364.241 |
| 10.1016/j.mtbio.2025.101690 | 29 | B | 0.227 | 44.177 | A | B | A | A | A | E | 96.0 | 1851.27 |
| 10.1016/j.mtbio.2025.101690 | 30 | B | 0.227 | 56.5916 | B | B | A | A | A | E | 96.0 | 1481.01 |
| 10.1016/j.mtbio.2025.101690 | 31 | B | 0.227 | 58.795 | B | B | A | A | A | E | 96.0 | 1063.29 |
| 10.1016/j.mtbio.2025.101690 | 32 | B | 0.227 | 68.073 | B | B | A | A | A | E | 96.0 | 669.304 |
| 10.1002/advs.202206771 | 33 | A | 0.8201 | 13.1805 | A | A | A | A | A | A | 24.0 | 775.76 |
| 10.1002/advs.202206771 | 34 | A | 0.9985 | 6.593 | B | A | A | A | A | A | 24.0 | 476.648 |
| 10.1002/btm2.10217 | 35 | C | — | 90.0 | A | D | A | C | B | C | 72.0 | 704.545 |
| 10.1002/btm2.10217 | 36 | C | — | 90.0 | B | D | A | C | B | C | 72.0 | 428.03 |
| 10.1002/btm2.10217 | 37 | C | — | 90.0 | A | D | A | C | D | C | 72.0 | 875.0 |
| 10.1002/btm2.10217 | 38 | C | — | 90.0 | B | D | A | C | D | C | 72.0 | 590.909 |
| 10.1002/btm2.10217 | 39 | C | — | 90.0 | A | D | A | C | C | C | 72.0 | 583.333 |
| 10.1002/btm2.10217 | 40 | C | — | 90.0 | B | D | A | C | C | C | 72.0 | 212.121 |
| 10.1021/acsami.4c18945 | 41 | A | — | 59.081 | A | A | B | A | A | A | 24.0 | 373.937 |
| 10.1021/acsami.4c18945 | 42 | A | 1.3 | 79.5045 | C | A | B | A | A | A | 24.0 | 248.824 |
| 10.1021/acsami.4c18945 | 43 | A | 1.3 | 80.389 | C | A | B | A | A | A | 24.0 | 162.299 |
| 10.1016/j.mtbio.2024.101340 | 44 | A | 0.42377 | 295.976 | B | A | B | A | A | A | 48.0 | 494.064 |
| 10.1016/j.mtbio.2024.101340 | 45 | A | 0.42377 | 295.976 | E | A | B | A | A | A | 48.0 | 383.374 |
| 10.1002/smll.202405236 | 46 | A | — | — | A | A | B | A | A | A | 48.0 | 69.9588 |
| 10.1002/smll.202405236 | 47 | A | — | — | B | A | B | A | A | A | 48.0 | 59.6367 |
| 10.1002/smll.202405236 | 48 | A | — | — | A | A | B | A | A | A | 48.0 | 64.9004 |
| 10.1002/smll.202405236 | 49 | A | — | — | B | A | B | A | A | A | 48.0 | 56.563 |
| 10.1002/adma.202108430 | 50 | B | 10.0 | 10.411 | A | D | B | B | E | F | — | 597.329 |
| 10.1002/adma.202108430 | 51 | B | 10.0 | 10.411 | B | D | B | B | E | F | — | 285.0 |
| 10.1002/adma.202108430 | 52 | B | 10.0 | 10.411 | D | D | B | B | E | F | — | 602.925 |
| 10.1002/adma.202108430 | 53 | B | 10.0 | 10.411 | C | D | B | B | E | F | — | 263.706 |
| 10.1016/j.colsurfb.2024.114466 | 54 | A | 3.5015 | 142.607 | B | A | A | C | A | A | 24.0 | 1096.31 |
| 10.1016/j.colsurfb.2024.114466 | 55 | A | 1.1265 | 142.607 | B | A | A | C | A | A | 24.0 | 1396.74 |
| 10.1007/s13770-022-00437-5 | 56 | B | 14.343 | 70.7182 | A | B | A | A | A | B | 24.0 | 0.182773 |
| 10.1007/s13770-022-00437-5 | 57 | B | 14.343 | 70.7182 | C | B | A | A | A | B | 24.0 | 0.0453782 |
| 10.1016/j.biomaterials.2025.123414 | 58 | A | 1.1178 | 133.677 | A | D | A | A | A | B | 24.0 | 237.242 |
| 10.1016/j.biomaterials.2025.123414 | 59 | A | 1.0371 | 189.967 | C | D | A | A | A | B | 24.0 | 42.9847 |
| 10.1016/j.biomaterials.2025.123376 | 60 | B | — | 123.179 | A | D | A | A | F | A | 24.0 | 229.627 |
| 10.1016/j.biomaterials.2025.123376 | 61 | B | — | — | B | D | A | A | F | A | 24.0 | 258.859 |
| 10.1016/j.biomaterials.2025.123376 | 62 | B | 1.3477 | 336.94 | E | D | A | A | F | A | 24.0 | 413.19 |
| 10.1016/j.jconrel.2025.113893 | 63 | A | 3.004 | 84.437 | A | A | B | A | A | B | 24.0 | 2627.21 |
| 10.1016/j.jconrel.2025.113893 | 64 | A | 3.004 | 84.437 | D | A | B | A | A | B | 24.0 | 2547.12 |
| 10.1016/j.jconrel.2025.113893 | 65 | A | 3.004 | 84.437 | D | A | B | A | A | B | 24.0 | 2379.86 |
| 10.1016/j.jconrel.2025.113893 | 66 | A | 3.004 | 84.437 | C | A | B | A | A | B | 24.0 | 2060.62 |
| 10.1038/s41467-026-68318-2 | 67 | A | 0.087 | 27.8 | C | B | A | A | E | F | 24.0 | 73.5981 |
| 10.1038/s41467-026-68318-2 | 68 | A | 0.2542 | 28.6 | F | B | A | A | E | F | 24.0 | 124.065 |
| 10.1038/s41467-026-68318-2 | 69 | A | 0.9287 | 19.8 | E | B | B | A | E | F | 24.0 | 206.075 |
| 10.1016/j.mtbio.2026.102863 | 70 | A | — | — | A | A | C | A | A | B | 24.0 | 50.2006 |
| 10.1016/j.mtbio.2026.102863 | 71 | A | — | 16.1591 | A | A | C | A | A | B | 24.0 | 47.6791 |
| 10.1016/j.mtbio.2026.102863 | 72 | A | — | 4.5605 | C | A | B | A | A | B | 24.0 | 24.0688 |
| 10.1186/s13018-025-06631-0 | 73 | A | 2.6997 | — | B | A | A | A | A | A | 24.0 | 70.4354 |
| 10.1186/s13018-025-06631-0 | 74 | A | 2.6997 | — | B | A | A | A | A | A | 24.0 | 147.016 |
| 10.1186/s12951-024-02810-z | 75 | A | — | 130.1491 | A | A | A | A | A | B | 24.0 | 642.424 |
| 10.1186/s12951-024-02810-z | 76 | A | 1.0 | 177.823 | B | A | A | A | A | B | 24.0 | 565.657 |
| 10.1093/burnst/tkaf024 | 77 | C | 1.0 | 88.58 | A | D | A | B | E | D | 192.0 | 506.456 |
| 10.1093/burnst/tkaf024 | 78 | C | — | 87.94 | C | D | A | B | E | D | 192.0 | 367.334 |
| 10.1093/burnst/tkaf024 | 79 | C | — | 87.94 | C | D | A | B | E | D | 192.0 | 215.074 |
| 10.1093/burnst/tkaf024 | 80 | C | — | 87.94 | C | D | A | B | E | D | 192.0 | 167.923 |
| 10.1021/acsnano.5c10123 | 81 | A | 1.59979 | 156.933 | C | A | A | A | A | A | 48.0 | 1803.7 |
| 10.1021/acsnano.5c10123 | 82 | A | 1.65229 | 200.938 | C | A | A | A | A | A | 48.0 | 1768.45 |
| 10.1016/j.mtbio.2026.102988 | 83 | A | 2.5039 | 84.4927 | A | A | A | B | E | D | 168.0 | 55.5102 |
| 10.1016/j.mtbio.2026.102988 | 84 | A | 5.4922 | 84.4927 | A | A | B | B | E | D | 168.0 | 41.4505 |
| 10.1016/j.mtbio.2026.102988 | 85 | A | 5.4922 | 84.4927 | C | A | B | B | E | D | 168.0 | 35.8554 |
| 10.1016/j.mtbio.2026.102988 | 86 | A | 5.4922 | 84.4927 | C | A | B | B | E | D | 168.0 | 33.8331 |
| 10.1016/j.mtbio.2025.102521 | 87 | A | 0.6287 | 10.0 | B | B | A | A | A | A | 18.0 | 142.697 |
| 10.1016/j.mtbio.2025.102521 | 88 | A | 0.6287 | 15.2632 | B | B | A | A | A | A | 18.0 | 110.451 |
| 10.1016/j.mtbio.2025.102521 | 89 | A | 0.6287 | 15.2632 | C | B | A | A | A | A | 18.0 | 108.078 |
| 10.1016/j.mtbio.2025.102519 | 90 | A | — | — | A | A | C | A | A | B | 8.0 | 191.547 |
| 10.1016/j.mtbio.2025.102519 | 91 | A | 0.0472 | 242.3805 | C | A | A | A | A | B | 8.0 | 125.485 |
| 10.1016/j.mtbio.2025.102519 | 92 | A | 0.097 | 159.96 | C | A | C | A | A | B | 8.0 | 181.02 |
| 10.1016/j.mtbio.2025.102519 | 93 | A | — | — | C | A | A | A | A | B | 8.0 | 103.18 |
| 10.1016/j.mtbio.2025.102556 | 94 | C | 0.883 | 18.98 | A | D | A | A | F | A | 12.0 | 304.806 |
| 10.1016/j.mtbio.2025.102556 | 95 | C | 0.883 | 16.783 | B | D | B | A | F | A | 12.0 | 284.309 |
| 10.1016/j.mtbio.2025.102556 | 96 | C | 0.883 | 10.043 | B | D | B | A | F | A | 12.0 | 236.606 |
| 10.1016/j.mtbio.2025.101810 | 97 | A | 0.8718 | 22.0221 | A | A | A | A | A | B | 24.0 | 112.421 |
| 10.1016/j.mtbio.2025.101810 | 98 | A | — | — | C | A | A | A | A | B | 24.0 | 100.105 |
| 10.1016/j.mtbio.2025.101810 | 99 | A | — | — | C | A | A | A | A | B | 24.0 | 87.4737 |
| 10.1016/j.mtbio.2025.101810 | 100 | A | 0.7565 | 22.1846 | C | A | A | A | A | B | 24.0 | 81.48 |
| 10.1016/j.mtbio.2024.100960 | 101 | A | 0.539 | 148.83 | A | D | A | A | A | B | 24.0 | 712.695 |
| 10.1016/j.mtbio.2024.100960 | 102 | A | — | 100.0 | A | D | B | A | A | B | 24.0 | 627.877 |
| 10.1016/j.mtbio.2024.100960 | 103 | A | — | 148.83 | B | D | A | A | A | B | 24.0 | 288.561 |
| 10.1016/j.mtbio.2024.100960 | 104 | A | 2.962 | 100.0 | B | D | B | A | A | B | 24.0 | 289.782 |
| 10.1016/j.mtbio.2023.100753 | 105 | B | 8.4838 | 100.0 | A | A | A | A | B | A | 48.0 | 283.688 |
| 10.1016/j.mtbio.2023.100753 | 106 | B | 7.2986 | 100.0 | A | A | B | A | B | A | 48.0 | 319.149 |
| 10.1016/j.mtbio.2023.100753 | 107 | B | 3.5545 | 100.0 | B | A | B | A | B | A | 48.0 | 215.603 |
| 10.1016/j.mtbio.2022.100392 | 108 | B | 19.2166 | 20.0 | A | A | B | A | B | A | 24.0 | 151.154 |
| 10.1016/j.mtbio.2022.100392 | 109 | B | 19.2166 | 20.0 | A | A | B | A | B | A | 24.0 | 140.769 |
| 10.1016/j.mtbio.2022.100392 | 110 | B | 19.2166 | 20.0 | B | A | B | A | B | A | 24.0 | 155.769 |
| 10.1016/j.mtbio.2022.100392 | 111 | B | 19.2166 | 20.0 | B | A | B | A | B | A | 24.0 | 148.846 |
| 10.1016/j.mtbio.2022.100392 | 112 | B | 19.2166 | 20.0 | B | A | B | A | B | A | 24.0 | 176.538 |
| 10.1016/j.mtbio.2022.100392 | 113 | B | 19.2166 | 20.0 | A | A | B | A | B | A | 72.0 | 180.0 |
| 10.1016/j.mtbio.2022.100392 | 114 | B | 19.2166 | 20.0 | A | A | B | A | B | A | 72.0 | 153.462 |
| 10.1016/j.mtbio.2022.100392 | 115 | B | 19.2166 | 20.0 | B | A | B | A | B | A | 72.0 | 158.077 |
| 10.1016/j.mtbio.2022.100392 | 116 | B | 19.2166 | 20.0 | B | A | B | A | B | A | 72.0 | 168.462 |
| 10.1016/j.mtbio.2022.100392 | 117 | B | 19.2166 | 20.0 | B | A | B | A | B | A | 72.0 | 184.615 |
| 10.1016/j.mtbio.2022.100392 | 118 | B | 19.2166 | 20.0 | A | A | B | A | B | A | 120.0 | 214.615 |
| 10.1016/j.mtbio.2022.100392 | 119 | B | 19.2166 | 20.0 | A | A | B | A | B | A | 120.0 | 191.538 |
| 10.1016/j.mtbio.2022.100392 | 120 | B | 19.2166 | 20.0 | B | A | B | A | B | A | 120.0 | 185.769 |
| 10.1016/j.mtbio.2022.100392 | 121 | B | 19.2166 | 20.0 | B | A | B | A | B | A | 120.0 | 208.846 |
| 10.1016/j.mtbio.2022.100392 | 122 | B | 19.2166 | 20.0 | B | A | B | A | B | A | 120.0 | 207.692 |
| 10.1016/j.actbio.2016.09.024 | 123 | A | 0.3 | 3.0 | A | C | A | B | B | A | 36.0 | 144.082 |
| 10.1016/j.actbio.2016.09.024 | 124 | A | 0.3 | 3.0 | A | C | A | B | B | A | 36.0 | 130.749 |
| 10.1016/j.actbio.2016.09.024 | 125 | A | 0.3 | 3.0 | A | C | A | B | D | A | 36.0 | 129.855 |
| 10.1016/j.actbio.2016.09.024 | 126 | A | 0.3 | 3.0 | A | C | A | B | D | A | 36.0 | 138.41 |
| 10.1016/j.actbio.2016.09.024 | 127 | A | 0.3 | 3.0 | A | C | A | B | C | A | 36.0 | 137.53 |
| 10.1016/j.actbio.2016.09.024 | 128 | A | 0.3 | 3.0 | A | C | A | B | C | A | 36.0 | 106.674 |
| 10.1016/j.actbio.2016.09.024 | 129 | A | 0.3 | 3.0 | A | C | A | B | E | A | 36.0 | 127.667 |
| 10.1016/j.actbio.2016.09.024 | 130 | A | 0.3 | 3.0 | A | C | A | B | E | A | 36.0 | 118.704 |
| 10.1016/j.mtbio.2025.102080 | 131 | B | 36.883 | 2.95 | B | B | B | A | A | B | 24.0 | 461.686 |
| 10.1016/j.mtbio.2025.102080 | 132 | B | 22.857 | 4.9 | B | B | B | A | A | B | 24.0 | 599.954 |
| 10.1016/j.mtbio.2025.102080 | 133 | B | 9.62045 | 8.54 | B | B | A | A | A | B | 24.0 | 647.617 |
| 10.1016/j.mtbio.2025.102080 | 134 | B | 7.0 | 26.3 | B | B | C | A | A | B | 24.0 | 934.435 |
| 10.1016/j.mtbio.2026.102989 | 135 | B | 8.659 | 40.55 | F | D | A | E | A | A | 24.0 | 980.0 |
| 10.1016/j.mtbio.2026.102989 | 136 | B | 8.659 | 40.55 | F | D | A | A | A | A | 24.0 | 403.196 |
| 10.1039/D5BM01187F | 137 | A | 0.2579 | — | A | A | C | D | F | A | 144.0 | 361.674 |
| 10.1039/D5BM01187F | 138 | A | 1.1957 | — | A | A | A | D | F | A | 144.0 | 354.176 |
| 10.1039/D5BM01187F | 139 | A | 4.4266 | — | A | A | B | D | F | A | 144.0 | 702.217 |

Table S8. Complete TNF-α dataset before imputation (n = 139).

| DOI | No. | Hydrogel composition | Modulus (kPa) | Pore size (µm) | Bioactive cue | Crosslink method | Crosslink level | Macrophage model | Activation stimulus | Exposure mode | Exposure time (h) | Measured IL-10 (pg/mL) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 10.1016/j.bioactmat.2024.07.015 | 1 | A | — | 182.8023 | A | D | A | A | F | A | 48.0 | 53.7037 |
| 10.1016/j.bioactmat.2024.07.015 | 2 | A | — | 182.8023 | A | D | A | A | F | A | 96.0 | 82.0988 |
| 10.1016/j.mtbio.2025.101686 | 3 | A | 19.1869 | 40.011 | A | A | B | A | A | B | 48.0 | 64.8354 |
| 10.1016/j.mtbio.2025.101686 | 4 | A | 16.8094 | 50.25 | C | A | B | A | A | B | 48.0 | 92.6978 |
| 10.1016/j.mtbio.2025.101686 | 5 | A | 13.1193 | 97.387 | C | A | B | A | A | B | 48.0 | 140.56 |
| 10.1038/s41467-024-50072-y | 6 | A | — | — | A | A | C | B | B | A | 24.0 | 63.7474 |
| 10.1038/s41467-024-50072-y | 7 | A | — | — | A | A | C | B | D | A | 24.0 | 205.237 |
| 10.1038/s41467-024-50072-y | 8 | A | — | — | A | A | C | B | E | A | 24.0 | 940.15 |
| 10.1038/s41467-024-50072-y | 9 | A | — | — | A | A | B | B | B | A | 24.0 | 49.9637 |
| 10.1038/s41467-024-50072-y | 10 | A | — | — | A | A | B | B | D | A | 24.0 | 61.7613 |
| 10.1038/s41467-024-50072-y | 11 | A | — | — | A | A | B | B | E | A | 24.0 | 784.833 |
| 10.1186/s12951-024-02996-2 | 12 | A | 12.263 | 142.614 | B | A | B | B | C | A | 24.0 | 396.255 |
| 10.1186/s12951-024-02996-2 | 13 | A | 16.1507 | 139.205 | B | A | B | B | C | A | 24.0 | 308.821 |
| 10.1186/s12951-024-02996-2 | 14 | A | 29.6548 | 117.045 | C | A | B | B | C | A | 24.0 | 760.713 |
| 10.1002/smll.202203680 | 15 | A | 0.0841 | — | A | B | C | B | E | C | 72.0 | 81.6 |
| 10.1002/smll.202203680 | 16 | A | 0.4281 | — | A | D | A | B | E | C | 72.0 | 108.8 |
| 10.1002/smll.202203680 | 17 | A | 0.4434 | — | A | D | A | B | E | C | 72.0 | 248.8 |
| 10.1002/smll.202203680 | 18 | A | 0.438 | — | A | D | A | B | E | C | 72.0 | 189.2 |
| 10.34133/bmr.0029 | 19 | A | 26.67 | 60.0 | A | D | A | A | F | F | — | 1.55869 |
| 10.34133/bmr.0029 | 20 | A | 36.67 | 60.0 | A | D | A | A | F | F | — | 2.02817 |
| 10.3389/fimmu.2023.1170153 | 21 | A | 0.752 | — | A | C | C | B | E | D | 72.0 | 60.9211 |
| 10.1016/j.actbio.2025.03.015 | 22 | B | 5.593 | 250.31 | A | A | B | A | A | A | 24.0 | 398.683 |
| 10.1016/j.actbio.2025.03.015 | 23 | B | 4.123 | 116.52 | B | A | B | A | A | A | 24.0 | 269.747 |
| 10.1016/j.mtbio.2025.101690 | 24 | B | 0.227 | 44.177 | A | B | A | A | A | E | 96.0 | 22.5485 |
| 10.1016/j.mtbio.2025.101690 | 25 | B | 0.227 | 56.5916 | B | B | A | A | A | E | 96.0 | 40.3391 |
| 10.1016/j.mtbio.2025.101690 | 26 | B | 0.227 | 58.795 | B | B | A | A | A | E | 96.0 | 92.9093 |
| 10.1016/j.mtbio.2025.101690 | 27 | B | 0.227 | 68.073 | B | B | A | A | A | E | 96.0 | 130.337 |
| 10.1002/btm2.10217 | 28 | C | — | 90.0 | A | D | A | C | B | C | 72.0 | 208.522 |
| 10.1002/btm2.10217 | 29 | C | — | 90.0 | B | D | A | C | B | C | 72.0 | 552.807 |
| 10.1002/btm2.10217 | 30 | C | — | 90.0 | B | D | A | C | D | C | 72.0 | 340.714 |
| 10.1002/btm2.10217 | 31 | C | — | 90.0 | A | D | A | C | C | C | 72.0 | 537.73 |
| 10.1002/btm2.10217 | 32 | C | — | 90.0 | B | D | A | C | C | C | 72.0 | 844.182 |
| 10.1021/acsami.4c18945 | 33 | A | — | 59.081 | A | A | B | A | A | A | 24.0 | 33.4879 |
| 10.1021/acsami.4c18945 | 34 | A | 1.3 | 79.5045 | C | A | B | A | A | A | 24.0 | 45.2363 |
| 10.1021/acsami.4c18945 | 35 | A | 1.3 | 80.389 | C | A | B | A | A | A | 24.0 | 78.7929 |
| 10.1016/j.mtbio.2024.101340 | 36 | A | 0.42377 | 295.976 | B | A | B | A | A | A | 48.0 | 451.811 |
| 10.1016/j.mtbio.2024.101340 | 37 | A | 0.42377 | 295.976 | E | A | B | A | A | A | 48.0 | 629.613 |
| 10.1002/smll.202405236 | 38 | A | — | — | A | A | B | A | A | A | 48.0 | 39.6917 |
| 10.1002/smll.202405236 | 39 | A | — | — | B | A | B | A | A | A | 48.0 | 47.687 |
| 10.1002/smll.202405236 | 40 | A | — | — | A | A | B | A | A | A | 48.0 | 40.5419 |
| 10.1002/smll.202405236 | 41 | A | — | — | B | A | B | A | A | A | 48.0 | 59.6115 |
| 10.1002/adma.202200521 | 42 | A | 507.772 | 45.107 | A | A | A | B | E | D | 168.0 | 53.4483 |
| 10.1002/adma.202200521 | 43 | A | 1139.9 | 27.228 | B | A | A | B | E | D | 168.0 | 66.8966 |
| 10.1002/adma.202200521 | 44 | A | 1523.32 | 17.8496 | B | A | B | B | E | D | 168.0 | 73.1034 |
| 10.1016/j.msec.2022.112721 | 45 | B | — | 0.8375 | D | D | B | A | E | C | 24.0 | 32.6525 |
| 10.1016/j.msec.2022.112721 | 46 | B | — | 0.8375 | D | D | B | A | E | C | 96.0 | 108.468 |
| 10.1016/j.msec.2022.112721 | 47 | B | — | 0.8375 | D | D | B | A | E | C | 168.0 | 150.226 |
| 10.1016/j.msec.2022.112721 | 48 | B | — | 0.8375 | D | D | B | A | E | C | 240.0 | 129.534 |
| 10.1016/j.msec.2022.112721 | 49 | B | — | — | D | D | B | A | E | C | 312.0 | 152.284 |
| 10.1016/j.msec.2022.112721 | 50 | B | — | — | A | D | B | A | E | C | 24.0 | 46.875 |
| 10.1016/j.msec.2022.112721 | 51 | B | — | — | A | D | B | A | E | C | 96.0 | 72.8059 |
| 10.1016/j.msec.2022.112721 | 52 | B | — | — | A | D | B | A | E | C | 168.0 | 74.2021 |
| 10.1016/j.msec.2022.112721 | 53 | B | — | — | A | D | B | A | E | C | 240.0 | 78.391 |
| 10.1016/j.msec.2022.112721 | 54 | B | — | — | A | D | B | A | E | C | 312.0 | 106.915 |
| 10.1016/j.ijbiomac.2024.129682 | 55 | A | 2.077 | 352.56 | A | D | A | A | A | B | 52.0 | 58.5145 |
| 10.1016/j.ijbiomac.2024.129682 | 56 | A | 1.595 | 295.68 | C | D | B | A | A | B | 52.0 | 250.082 |
| 10.1016/j.ijbiomac.2024.129682 | 57 | A | 1.105 | 283.45 | C | D | B | A | A | B | 52.0 | 369.809 |
| 10.1016/j.ijbiomac.2024.129682 | 58 | A | 1.052 | 161.559 | C | D | B | A | A | B | 52.0 | 414.666 |
| 10.1016/j.colsurfb.2024.114466 | 59 | A | 3.5015 | 142.607 | B | A | A | C | A | A | 24.0 | 146.873 |
| 10.1016/j.colsurfb.2024.114466 | 60 | A | 1.1265 | 142.607 | B | A | A | C | A | A | 24.0 | 101.321 |
| 10.1007/s13770-022-00437-5 | 61 | B | 14.343 | 70.7182 | A | B | A | A | A | B | 24.0 | 0.0544743 |
| 10.1007/s13770-022-00437-5 | 62 | B | 14.343 | 70.7182 | C | B | A | A | A | B | 24.0 | 0.141685 |
| 10.1016/j.biomaterials.2025.123414 | 63 | A | 1.1178 | 133.677 | A | D | A | A | A | B | 24.0 | 7.07635 |
| 10.1016/j.biomaterials.2025.123414 | 64 | A | 1.0371 | 189.967 | C | D | A | A | A | B | 24.0 | 16.0521 |
| 10.1016/j.biomaterials.2025.123376 | 65 | B | — | 123.179 | A | D | A | A | F | A | 24.0 | 94.4699 |
| 10.1016/j.biomaterials.2025.123376 | 66 | B | — | — | B | D | A | A | F | A | 24.0 | 109.133 |
| 10.1016/j.biomaterials.2025.123376 | 67 | B | 1.3477 | 336.94 | E | D | A | A | F | A | 24.0 | 101.031 |
| 10.1016/j.jconrel.2025.113893 | 68 | A | 3.004 | 84.437 | A | A | B | A | A | B | 24.0 | 1251.61 |
| 10.1016/j.jconrel.2025.113893 | 69 | A | 3.004 | 84.437 | D | A | B | A | A | B | 24.0 | 1600.0 |
| 10.1016/j.jconrel.2025.113893 | 70 | A | 3.004 | 84.437 | D | A | B | A | A | B | 24.0 | 1458.06 |
| 10.1016/j.jconrel.2025.113893 | 71 | A | 3.004 | 84.437 | C | A | B | A | A | B | 24.0 | 1780.65 |
| 10.1038/s41467-026-68318-2 | 72 | A | 0.087 | 27.8 | C | B | A | A | E | F | 24.0 | 68.8742 |
| 10.1038/s41467-026-68318-2 | 73 | A | 0.2542 | 28.6 | F | B | A | A | E | F | 24.0 | 49.647 |
| 10.1038/s41467-026-68318-2 | 74 | A | 0.9287 | 19.8 | E | B | B | A | E | F | 24.0 | 31.8951 |
| 10.1016/j.mtbio.2026.102863 | 75 | A | — | — | A | A | C | A | A | B | 24.0 | 10.5823 |
| 10.1016/j.mtbio.2026.102863 | 76 | A | — | 16.1591 | A | A | B | A | A | B | 24.0 | 11.6035 |
| 10.1016/j.mtbio.2026.102863 | 77 | A | — | 4.5605 | C | A | B | A | A | B | 24.0 | 15.1096 |
| 10.1186/s13018-025-06631-0 | 78 | A | 2.6997 | — | B | A | A | A | A | A | 24.0 | 36.8228 |
| 10.1186/s13018-025-06631-0 | 79 | A | 2.6997 | — | B | A | A | A | A | A | 24.0 | 26.0622 |
| 10.1186/s12951-024-02810-z | 80 | A | — | 130.1491 | A | A | A | A | A | B | 24.0 | 44.7558 |
| 10.1186/s12951-024-02810-z | 81 | A | 1.0 | 177.823 | B | A | A | A | A | B | 24.0 | 48.5897 |
| 10.1021/acsnano.5c10123 | 82 | A | 1.59979 | 156.933 | C | A | A | A | A | A | 48.0 | 112.587 |
| 10.1021/acsnano.5c10123 | 83 | A | 1.65229 | 200.938 | C | A | A | A | A | A | 48.0 | 124.476 |
| 10.1016/j.mtbio.2025.102521 | 84 | A | 0.6287 | 10.0 | B | B | A | A | A | A | 18.0 | 109.393 |
| 10.1016/j.mtbio.2025.102521 | 85 | A | 0.6287 | 15.2632 | B | B | A | A | A | A | 18.0 | 127.944 |
| 10.1016/j.mtbio.2025.102521 | 86 | A | 0.6287 | 15.2632 | C | B | A | A | A | A | 18.0 | 125.051 |
| 10.1016/j.mtbio.2025.102556 | 87 | C | 0.883 | 18.98 | A | D | A | A | F | A | 12.0 | 11.9538 |
| 10.1016/j.mtbio.2025.102556 | 88 | C | 0.883 | 16.783 | B | D | B | A | F | A | 12.0 | 15.6916 |
| 10.1016/j.mtbio.2025.102556 | 89 | C | 0.883 | 10.043 | B | D | B | A | F | A | 12.0 | 72.8542 |
| 10.1016/j.mtbio.2025.102174 | 90 | B | 0.3384 | 53.392 | B | D | B | A | A | A | — | 52.5753 |
| 10.1016/j.mtbio.2025.102174 | 91 | B | 0.5233 | 34.971 | B | D | B | A | A | A | — | 53.1773 |
| 10.1016/j.mtbio.2024.100960 | 92 | A | 0.539 | 148.83 | A | D | A | A | A | B | 24.0 | 277.026 |
| 10.1016/j.mtbio.2024.100960 | 93 | A | — | 100.0 | A | D | B | A | A | B | 24.0 | 261.927 |
| 10.1016/j.mtbio.2024.100960 | 94 | A | — | 148.83 | B | D | A | A | A | B | 24.0 | 459.479 |
| 10.1016/j.mtbio.2024.100960 | 95 | A | 2.962 | 100.0 | B | D | B | A | A | B | 24.0 | 509.658 |
| 10.1016/j.mtbio.2023.100753 | 96 | B | 8.4838 | 100.0 | A | A | A | A | B | A | 48.0 | 357.007 |
| 10.1016/j.mtbio.2023.100753 | 97 | B | 7.2986 | 100.0 | A | A | B | A | B | A | 48.0 | 382.434 |
| 10.1016/j.mtbio.2023.100753 | 98 | B | 3.5545 | 100.0 | B | A | B | A | B | A | 48.0 | 445.205 |
| 10.1016/j.mtbio.2022.100392 | 99 | B | 19.2166 | 20.0 | A | A | B | A | B | A | 24.0 | 109.944 |
| 10.1016/j.mtbio.2022.100392 | 100 | B | 19.2166 | 20.0 | A | A | B | A | B | A | 24.0 | 98.1033 |
| 10.1016/j.mtbio.2022.100392 | 101 | B | 19.2166 | 20.0 | B | A | B | A | B | A | 24.0 | 92.9424 |
| 10.1016/j.mtbio.2022.100392 | 102 | B | 19.2166 | 20.0 | B | A | B | A | B | A | 24.0 | 87.0424 |
| 10.1016/j.mtbio.2022.100392 | 103 | B | 19.2166 | 20.0 | B | A | B | A | B | A | 24.0 | 81.885 |
| 10.1016/j.mtbio.2022.100392 | 104 | B | 19.2166 | 20.0 | A | A | B | A | B | A | 72.0 | 84.2009 |
| 10.1016/j.mtbio.2022.100392 | 105 | B | 19.2166 | 20.0 | A | A | B | A | B | A | 72.0 | 96.1225 |
| 10.1016/j.mtbio.2022.100392 | 106 | B | 19.2166 | 20.0 | B | A | B | A | B | A | 72.0 | 88.7339 |
| 10.1016/j.mtbio.2022.100392 | 107 | B | 19.2166 | 20.0 | B | A | B | A | B | A | 72.0 | 89.5171 |
| 10.1016/j.mtbio.2022.100392 | 108 | B | 19.2166 | 20.0 | B | A | B | A | B | A | 72.0 | 99.2092 |
| 10.1016/j.mtbio.2022.100392 | 109 | B | 19.2166 | 20.0 | A | A | B | A | B | A | 120.0 | 105.238 |
| 10.1016/j.mtbio.2022.100392 | 110 | B | 19.2166 | 20.0 | A | A | B | A | B | A | 120.0 | 106.762 |
| 10.1016/j.mtbio.2022.100392 | 111 | B | 19.2166 | 20.0 | B | A | B | A | B | A | 120.0 | 121.656 |
| 10.1016/j.mtbio.2022.100392 | 112 | B | 19.2166 | 20.0 | B | A | B | A | B | A | 120.0 | 117.983 |
| 10.1016/j.mtbio.2022.100392 | 113 | B | 19.2166 | 20.0 | B | A | B | A | B | A | 120.0 | 121.733 |
| 10.1016/j.mtbio.2025.102276 | 114 | A | 11.2329 | 5.3 | E | A | A | A | A | B | 6.0 | 632.062 |
| 10.1016/j.mtbio.2025.102276 | 115 | A | 9.31507 | 6.34 | C | A | A | A | A | B | 6.0 | 1090.91 |
| 10.1016/j.mtbio.2025.102276 | 116 | A | 11.2329 | 5.3 | E | A | A | A | A | B | 12.0 | 630.176 |
| 10.1016/j.mtbio.2025.102276 | 117 | A | 9.31507 | 6.34 | C | A | A | A | A | B | 12.0 | 1100.43 |
| 10.1016/j.mtbio.2025.102276 | 118 | A | 11.2329 | 5.3 | E | A | A | A | A | B | 24.0 | 656.982 |
| 10.1016/j.mtbio.2025.102276 | 119 | A | 9.31507 | 6.34 | C | A | A | A | A | B | 24.0 | 1178.78 |
| 10.1016/j.actbio.2016.09.024 | 120 | A | 0.3 | 3.0 | A | C | A | B | B | A | 36.0 | 1216.58 |
| 10.1016/j.actbio.2016.09.024 | 121 | A | 0.3 | 3.0 | A | C | A | B | B | A | 36.0 | 1132.42 |
| 10.1016/j.actbio.2016.09.024 | 122 | A | 0.3 | 3.0 | A | C | A | B | D | A | 36.0 | 1163.72 |
| 10.1016/j.actbio.2016.09.024 | 123 | A | 0.3 | 3.0 | A | C | A | B | D | A | 36.0 | 1221.7 |
| 10.1016/j.actbio.2016.09.024 | 124 | A | 0.3 | 3.0 | A | C | A | B | C | A | 36.0 | 1096.3 |
| 10.1016/j.actbio.2016.09.024 | 125 | A | 0.3 | 3.0 | A | C | A | B | C | A | 36.0 | 1117.83 |
| 10.1016/j.actbio.2016.09.024 | 126 | A | 0.3 | 3.0 | A | C | A | B | E | A | 36.0 | 1101.77 |
| 10.1016/j.actbio.2016.09.024 | 127 | A | 0.3 | 3.0 | A | C | A | B | E | A | 36.0 | 1159.74 |
| 10.1039/D4BM01062K | 128 | A | 6.7 | — | A | A | A | B | A | A | 48.0 | 12.5 |
| 10.1039/D4BM01062K | 129 | A | 6.4 | 16.0 | A | A | A | B | A | A | 48.0 | 52.9762 |
| 10.1039/D4BM01062K | 130 | A | 6.5 | 9.0 | A | A | A | B | A | A | 48.0 | 45.8333 |
| 10.1039/D5BM01187F | 131 | A | 0.2579 | — | A | A | C | D | F | A | 144.0 | 224.622 |
| 10.1039/D5BM01187F | 132 | A | 1.1957 | — | A | A | A | D | F | A | 144.0 | 60.3054 |
| 10.1039/D5BM01187F | 133 | A | 4.4266 | — | A | A | B | D | F | A | 144.0 | 104.154 |

Table S9. Complete IL-10 dataset before imputation (n = 133).

Figure S1. Measured versus predicted TNF-α (a) and IL-10 (b) concentrations. Training points show pooled out-of-fold predictions and Test points show predictions from Training-only models. Shading indicates ±20% and ±50% relative error.

Figure S2. TNF-α SHAP landscapes coloured by (a) hydrogel composition, (b) modulus, (c) pore size, (d) bioactive cue, (e) crosslink method and (f) crosslink level. Ten-neighbour trustworthiness is 0.924. Numerical colour scales are logarithmic; grey denotes missing or non-positive values.

Figure S3. IL-10 SHAP landscapes coloured by (a) hydrogel composition, (b) modulus, (c) bioactive cue, (d) crosslink method, (e) crosslink level and (f) activation stimulus. Ten-neighbour trustworthiness is 0.977. Modulus uses a logarithmic colour scale; grey denotes missing or non-positive values.

Figure S4. SHAP landscapes coloured by macrophage model, exposure mode and exposure time (h): (a–c) TNF-α and (d–f) IL-10. Coordinates correspond to Figures S2–S3; missing exposure-time values are shown in grey.